Odesa National Medical University

Department of paediatric dentistry

METHODICAL RECOMMENDATIONS

for students

Academic discipline: “ Propaedeutics of pediatric dentistry”

Lesson №10 “Materials for filling: Modern qualification of dental materials .

Constituents , properties and method of use.

Their types, settings. Technique of use.

Filling of carious cavities 2 class by Black in the temporary and permanent teeth in children with different filling materials”

Course 2. Faculty of Dentistry

Speciality.   221 “Dentistry”

«Затверджено»

На методичній нараді кафедри

стоматології дитячого віку

протокол № ___ від ______2021р.

Зав. кафедрою ________проф. О.В.Дєньга

Odessa   - 2021

Materials for filling: Modern qualification of dental materials .

Constituents , properties and method of use.

Their types, settings. Technique of use.

Filling of carious cavities 2, 3 and 4 classes by Black in the temporary and permanent teeth in children.

Concrete aims.

To show out main principles of stopping of carious cavities of II of class;

To take apart errors at stopping of cavities of II of class;

To learn the features of stopping of contiguous cavities of II of class;

To learn to application of matrix in the cavities of II of class;

To tell materials for stopping of carious cavities of II of class;

To tell materials for stopping of carious cavities of III of class;

To learn to application of matrix in the cavities of III of class;

To learn the features of stopping of contiguous cavities of III of class;

To understand determination of color of stopping material for stopping of cavities of IV of class ;

To memorize the sequence of stopping of cavities of IV of class;

To learn to forming of pin point in the cavities of IV of class;

To learn to forming of pin point in the cavities of IV of class;

To tell materials for stopping of carious cavities of IV of class;

To understand finish treatment of stopping;

To memorize stopping materials for the temporal teeth of II, III and IV of classes ;

To master the stages of stopping of cavities of II of class ;

To master the stages of stopping of cavities of III and IV of classes

2.Base level of preparation.

| Name of previous disciplines | Gained knowledge, abilities, skills |
| --- | --- |
| 1. Propedeutics of therapeutic stomatology | 1. Technique of preparing of carious cavities 2, 3 and 4 classes ; 2. Classification of stomatological material is for stopping of teeth. |

3. Organization of maintenance educational to the module.

1. Main principles of stopping of carious cavities of II of class;

2. Errors are at stopping of cavities of II of class;

3. Features of stopping of contiguous cavities of II of class;

4. Application of matrix is in the cavities of II of class;

5. Materials are for stopping of carious cavities of II of class;

6. Materials are for stopping of carious cavities of III of class;

7. Application of matrix is in the cavities of III of class;

8. Features of stopping of contiguous cavities of III of class;

9.    Determination of color of stopping material is for stopping of cavities of IV of class ;

10.Sequence of stopping of cavities of IV of class;

11.  Forming of pin point is in the cavities of IV of class;

12.  Materials are for stopping of carious cavities of IV of class;

13.  Finish of treatment of stopping;

14. Stopping materials for the temporal teeth of II, III and IV of classes ;

15. The stages of stopping of cavities of II of class ;

16. The stages of stopping of cavities of III and IV of classes .

4. Table of contents educational to the module.

STOPPING OF CARIOUS CAVITIES OF II OF CLASS.

The correct stopping of cavities of 2 classes is considered one of the most difficult tasks : there are most difficulties exactly at proceeding in the pin surfaces of teeth. It is related to that that in a norm the sides of intact teeth densely fit closely to each other, forming the so-called pin point. For the correct design of pin surface of tooth it is necessary to adhere to the stages of stopping and pay attention to next elements:

opening of three-cornered form is between teeth in a придесневой area, which in a norm is filled by a gingival papilla;

actually pin point which is localized in area of equator;

pin devil-fish of regional comb of tooth.

The most widespread errors which arise up at stopping of cavities of 2 classes include:

Absence of dense contact is between stopping and nearby tooth which results in the permanent hit of meal in an interdental interval and injuring of interdental papilla;

There is forming of pin point in area of regional comb of tooth, but not at the level of equator which results in відколів of stopping material;

Surplus introduction of material to the area of gingival wall of cavity is creation of "overhanging edge" what serves as reason of permanent trauma of interdental papilla and development of pocket in remote terms;

Absence of good adaptation of material is to the gingival wall which results in development of secondary caries.

Considerable difficulties are presented by stopping of contiguous cavities at an ashen edge (1) or at distribution of carious cavity under gums (2).

1.

Insulating gaskets in both cavities lay on at the first visit to the patients of stomatological cabinet;

stop carious cavities separately: stop one cavity

2.

Contiguous carious cavities which spread under gums, at inflammation of interdental papilla prepare simultaneously and treat a papillitis.

In further in both cavities lay on the temporal stopping, but, that they did not injure an interdental papilla.

In a 2-3 twenty-four hours when inflammation disappears, the temporal stopping replace permanent, picking up thread a pin point.

If for stopping of carious cavities of 2 classes apply high-early-strength stopping materials, a matrix must be removed from an interdental interval to consolidation of material as after consolidation of material creating a pin point is impossible.

Application of matrix during stopping:

Assists retaining of material in a cavity during his condensation;

Improves adaptation of material in area of gingival wall;

Provides creation correct to the contour of pin surface;

In a number of cases if a matrix is densely pulled-in round the neck of tooth of матрицетримача, guards from the hit of blood and gingival liquid.

Imposition of matrix :

Matrices can have a different design. A matrix with the special ear is used in cases, if the gingival wall of cavity is subjacent level of gums. In some cases, at large destruction of коронкової part of tooth it will be to use матрицетримач. For correct renewal of pin point interdental кліни of different sizes is needed. They densely pin a matrix ribbon against the tissues of tooth providing fixing of matrix and preventing education overhangs to the edge of material in an interdental interval.

Wedges are a plastic and wooden. By means of wedges it is possible to conduct "previous розклинювання". A wedge is entered between interdental by a papilla and matrix providing the dense fitting closely of matrix to the tooth: the three-cornered crossing of wedge must answer a form and size of interdental papilla. Getting wet, a wedge distends and slightly moves apart teeth.

At stopping of cavities of 2 classes, even in devital teeth, it is necessary to conduct anaesthetizing, as imposition of matrix carrer or introduction of wedge is sickly for a patient.

The pin surface of tooth is correctly formed nowise can not be flat - she has a form near to spherical. The zone of contact between teeth must be situated in area of equator and barely higher - as in intact teeth. A widespread error is a design of pin point at the level of regional combs of teeth : in this case except sticking of meal in an interdental interval possible since to material which the executed stopping is from. As a rule, these errors are constrained with the use of flat matrix what does not have a protuberant contour in area of equator.

Forming of pin devil-fish of regional comb comes true by means of shtrips or disks of "Sof-Lex". The presence of devil-fish of regional comb prevents since material in this area .

Materials:

At stopping of cavities of 2 classes traditionally apply composite materials of class of hybrids, compos that packed and amalgam. In connection with the increased aesthetic requirements an amalgam is used mainly for stopping of molars.

STOPPING OF CARIOUS CAVITIES OF III OF CLASS.

At stopping of cavities of 3 classes it is necessary to aspire a pin point to correct renewal, that maybe only at the use of contour matrices outbowed on a plane, and interdental wedges.

Materials:

Choosing material for stopping of cavities of 3 classes, it follows to take into account : placing of tooth and his "participating" in a smile, sizes and localization of carious cavity, aesthetic requirements of patient and him economic feasibilities.

For stopping of cavities of 3 classes it is possible to use compos, compomers, ionomer cements and amalgam.

Composite materials, compomers allow to provide the most aesthetic result;

Ionomer cements it follows to apply or in the cases when it is impossible stainsing of tissues of tooth, or on the economic considering.

An amalgam can be used for stopping of small cavities of 3 classes at the dog-teeth prepared by the "use of language access.

Stopping of carious cavity of 3 classes at presence of nearby tooth conduct with the obligatory use of rectangular matrices, if a carious cavity is located at the level of equator of crown of the tooth, and figured if she is below equator at the level of interdental papilla, or when a cavity spreads under gums.

Methodology of using a matrix :

After imposition of insulating gasket a matrix is fixed by means of wedge which is entered between healthy teeth and matrix.

Then bring in stopping material in a carious cavity, condense abandoning above carious a cavity insignificant surplus.

As soon as stopping begins to harden, a matrix is deleted,  decline sdws healthy (nearby) tooth and in vertical direction delete.

Surplus of stopping mass above stopping of деконденсують displacing her sdws healthy tooth, and form a pin point. Surface of stopping and tooth must be at one level, that the overpriced bite was not.

- At stopping of two contiguous carious cavities of 3 classes after the simultaneous preparing of cavity and closing of her temporal stopping treat inflammation of interdental papilla.

- After the removal of inflammation of papilla the temporal stopping treatments of teeth delete and continue.

- That saliva did not get in a carious cavity, in a ясневу furrow enter wadding туруну.

- Carious cavities dry out then.

- Lay on insulating gaskets which evenly cover a bottom and walls to enamel-dentinal to the border.

- By means of the еталона colourings at natural illumination pick up the color of stopping material is stopping must answer aesthetic requirements.

- Stopping material at first is brought in one carious cavity with small surplus.

- A celluloid matrix is entered between teeth, press down to the tooth from stopping materials and form the edge of stopping thus. The surface of stopping on a side must have a small bulge. Such bulges of both contiguous teeth create a pin point afterwards.

- After consolidation of stopping stopping mass is brought in the carious cavity of other tooth and carry out all stages of the described operation.

- Delete wadding turundas and matrix, by easy pressure on stopping take her to the contact with the surface of stopping of nearby tooth; delete surplus of stopping material from an interdental interval, check up the regional fitting closely of stopping in the приясенній area of walls.

- Polish and polish stopping in the next visit of patient.

STOPPING OF CARIOUS CAVITIES OF IV OF CLASS.

Complication of stopping of carious cavities of 4 classes consists in proceeding in a cutting edge, especially corner of crown.

Determination of color :

Taking into account the increased aesthetic requirements to stopping of cavities of 4 classes it is necessary to be more detailed stopped for determination of color of stopping material. A doctor must choose a few tints of опака (opaque compo) - for пришиїчної and pin parts of stopping, for a cutting edge, combination of which will give a necessary colour effect.

Determining a color follows at daily illumination or by the light of the field lamp. The lamp of the stomatological setting, if she gives a rather yellow color, it must turn off. A tooth before determination of color it follows to clean from a raid and delete the tissues and bits and pieces of the old stopping changed in a color. It is impossible to determine the color of tooth, if the tissues of tooth are hard-cured, are they always lighter. Choosing a tint, it is necessary to remember that an important role is played by the tint of tissues which a compo is laid on.

Stopping of cavities of 4 classes it is recommended to carry out in such sequence:

Proceeding in the contours of dentine from opac, composite material or ionomer;

Forming of language surface is by means of celluloid matrix and interdental wedge;

Forming of vestibular part of stopping, beginning from a neck area.

Pin point:

The necessary condition of success is the correct forming of pin point : in a norm he must begin wherein an interdental papilla is closed. If to form him nearer to the gingival edge, then a compo will press on an interdental papilla, causing pain and causing his inflammation. At the location of pin point only in area of cutting edges patients usually grumble about splashing of saliva at conversation.

The construction of cutting edge from composite materials always takes place in two stages:

1. Forming of language fragment of cutting edge. The first light-striking is conducted through an enamel or before imposed compo from a vestibular side;

2. Forming of vestibular fragment of cutting edge; a light-striking is conducted through a hardening language fragment.

Materials:

The high loading on the corner of crown part of tooth and increased aesthetic requirements is determined choice of stopping materials - compos of class of hybrids. Combining is assumed: language fragment of restoration and cutting edge - from a hybrid compo and vestibular fragment - from the compo of class of microfils, that excellent half own and by the protracted maintenance of brilliance. Application of compomers and ормокерів also fully possibly, as all necessary properties are inherent them however them polish and ability to keep brilliance lose to the compos of class of microfil.

Finish treatment:

Quality of stopping in remote terms in a great deal depends on correct finish treatment: only polishing of surface of compo to "dry brilliance" comparable with brilliance of natural enamel will prevent painting of stopping food pigments (and for women - by lipstick). For the receipt of "dry brilliance" it is necessary to restrain all stages of final treatment of the composite stopping. Application of encapsulant  improves stability of color of compo in the conditions of cavity of mouth.

STOPPING OF CARIOUS CAVITIES

IN TEMPORAL TEETH.

The choice of stopping material at treatment of temporal teeth depends on localization carious cavity and stages of development of tooth.

II CLASS

For stopping cavity of II of class a preference it follows to render to the silver amalgam, composite materials, склоіономерним cements, compomers.

On stopping there is the considerable masticatory loading in the cavity of II of class, that is why material for her must rubble first of all mechanically proof. The cement stopping in most cases does not maintain навантаженості и is broken off in the place of transition of basic cavity in auxiliary.

II, IV CLASS

At stopping каріозніх cavity of III, IV, V of classes ionomer cements, compomers and composition materials, are used in temporal teeth.

At stopping of carious cavities in temporal teeth which are on the stage of resorption of root next to the enumerated stopping materials can be used :  Zn-fosforic cements (phosphate-cement,Adhesor), Zn-fosfaric cements with the bactericidal including (phosphate-cement which contain silver, Argil) and polycarboxylate cements.

4. Table of contents of educational material

In the treatment of Dental Caries, it is important to make a distinction between

  - To treat the disease causing cavities

  - To treat (fill) the cavities which are the result of the disease

To treat the disease, the general approach we recommend is to

  - Identify the factors causing the disease

  - Install targeted actions against main etiological factors

  - Check that actions have been successful (evaluation)

  - We consider the treatment of the disease as a most important measure. If cavities are filled, and no measures against an ongoing disease are taken, there is a considerable risk for new cavities, for example at the margins of the fillings ("secondary caries"). To treat the disease, the same strategy as for prevention of caries can be used.

Regarding treatment of cavities - by fillings, inlays etc, a new section is under preparation.

A dental restoration or dental filling is a dental restoration  used to restore the function, integrity and morphology of missing tooth structure. The structural loss typically results from caries or external trauma. It is also lost intentionally during tooth preparation to improve the aesthetic or the physical integrity of the intended restorative material.

A tooth preparation is the finished product of a tooth's structure prior to restoration with a dental restorative material, such as gold , amalgam, composite, porcelain or any number of other materials.

Tooth preparation is usually required before placing a dental restoration. This process involves cutting the tooth usually with a dental drill to make space for the planned restoration, remove any dental decay and structurally unsound tooth. If permanent restoration can not be carried out after tooth preparation, temporary restoration is done.

There are two types of preparations.

- Intracoronal preparations are those preparations which serve to hold restorative material within the confines of the structure of the crown of a tooth. Examples include all classes of cavity preparations for composite or amalgam, as well as those for gold and porcelain inlays. Intracoronal preparations are also made as female recipients to receive the male components of RPDs.

- Extracoronal preparations are those preparations which serve as a core or base upon which or around which restorative material will be placed to bring the tooth back into a functional or esthetic structure. Examples include crowns and onlays, as well as veneers.

In preparing a tooth for a restoration, a number of considerations will come into play to determine the type and extent of the preparation. The most important factor to consider is decay. For the most part, the extent of the decay will define the extent of the preparation, and in turn, the subsequent method and appropriate materials for restoration.

Another consideration is unsupported tooth structure. In the photo at right, unsupported enamel can be seen where the underlying dentin was removed because of infiltrative decay. When preparing the tooth to receive a restoration, unsupported enamel is removed to allow for a more predictable restoration. While enamel is the hardest substance in the human body, it is particularly brittle, and unsupported enamel fractures easily.

### Dental restorations

Most dental restorations involve the removal of enamel. Frequently, the purpose of removal is to gain access to the underlying decay in the dentin or inflammation in the pulp. This is typically the case in amalgam restorations and endodontic teatment.

Nonetheless, enamel can sometimes be removed before there is any decay present. The most popular example is the dental sealant. The process of placing dental sealants in the past involved removing enamel in the deep fissures and grooves of a tooth and replacing it with a restorative material. Presently, it is more common to only remove decayed enamel if present. In spite of this, there are still cases where deep fissures and grooves in enamel are removed in order to prevent decay, and a sealant may or may not be placed depending on the situation. Sealants are unique in that they are preventative restorations for protection from future decay and have shown to reduce the risk of decay by 55% over 7 years.

Aesthetics is another reason for the removal of enamel. Removing enamel is necessary when placing crowns and veneers to enhance the appearance of teeth. In both of these instances, it is important to keep in mind the orientation of enamel rods because it is possible to leave enamel unsupported by underlying dentin, leaving that portion of the prepared teeth more vulnerable to fracture.

### Acid-etching techniques

Invented in 1955, acid-etching employs dental etchants and is used frequently when bonding dental restoration to teeth. This is important for long-term use of some materials, such as composites and sealants. By dissolving minerals in enamel, etchants remove the outer 10 micrometers on the enamel surface and make a porous layer 5–50 micrometers deep. This roughens the enamel microscopically and results in a greater surface area on which to bond.

The effects of acid-etching on enamel can vary. Important variables are the amount of time the etchant is applied, the type of etchant used, and the current condition of the enamel.

There are three types of patterns formed by acid-etching.[ Type 1 is a pattern where predominantly the enamel rods are dissolved; type 2 is a pattern where predominantly the area around the enamel rods are dissolved; and type 3 is a pattern where there is no evidence left of any enamel rods. Besides concluding that type 1 is the most favorable pattern and type 3 the least, the explanation for these different patterns is not known for certain but is most commonly attributed to different crystal orientation in the enamel.

### Tooth colored

Dental composites are also called white fillings, used in direct fillings. Crowns and in-lays can also be made in the laboratory from dental composites. These materials are similar to those used in direct fillings and are tooth coloured. Their strength and durability is not as high as porcelain or metal restorations and they are more prone to wear and discolouration.

Composite resin

Dental composites, also called white fillings, are a group of restorative materials used in dentistry. As with other composite materials, a dental composite typically consists of a resin-based matrix, such as a bisphenol A-glycidyl methacrylate BISMA resin like urethane dimethacrylate (UDMA), and an inorganic filler such as silicon dioxide silica. Compositions vary widely, with proprietary mixes of resins forming the matrix, as well as engineered filler glasses and glass ceramics. The filler gives the composite wear resistance and translucency. A coupling agent such as silane is used to enhance the bond between these two components. An initiator package begins the polymerization reaction of the resins when external energy (light/heat etc.) is applied. A catalyst package can control its speed. This is not recommended for molars.

After tooth preparation, a thin glue or bonding material layer is applied. Composites are then filled layer by layer and photo-polymerising each using light. At the end the surface will be shaped and polished.

COMPOSITE RESIN RESTORATIONS

General.

Composite resin is commonly used as a restorative material in anterior teeth because of its resistance to wear and its excellent aesthetics. The design of the cavity preparation will differ from the design of the amalgam, but most of the dental assistant's duties will be the same as those when amalgam is used. See figure 2-32 for steps of procedure when preparing restorations made of composite resin.

Varieties of Matrices:

Composite resin restorations require some kind of matrix to hold, shape, and protect them against stain and moisture contamination. Metal matrices, if used in conjunction with resin restorations, would stain the resin. Celluloid, which is issued in roll form, is normally the matrix of choice for proximal restorations. The celluloid matrix strip is approximately three-eighths of an inch wide and is cut to the desired length. Another celluloid-type matrix that is used with resin restorations is the cervical matrix. It is cylindrical or tabular in shape and is generally used on the facial and lingual surfaces of anterior teeth. This matrix offers the same protection against contamination, as do the celluloid strips. Crown forms are also made of celluloid and are shaped to match the morphology of the tooth. They come in numbered sets that vary in size, depending on the size and shape of the tooth involved. These crowns may also be used to prepare a temporary crown, to contain a sedative filling, or as a matrix for other types of restoration. If necessary, these crown forms may be modified and cut to fit the tooth being worked on. In order to hold many of these matrices in place and help them conform to an irregularly shaped tooth, a small wedge of wood is commonly available. Thus, we will always include a selection of wooden wedges in any setup.

Mixing Composite Resins.

Composite resins have largely replaced unfilled acrylic resins, because they last longer and have more desirable properties. They usually have a calcium hydroxide base. They are also very simple to mix and use. Most of these restorative kits contain the mixing instructions and mixing materials. If a crown form is not used to place the material, a plastic-coated plugger may be used. In using any of the compo- sites, it is always wise to follow the manufacturer's instructions. Failure to do so may result in a faulty restoration.

Completing the Restoration.

If resin is the restorative material, the matrix will be removed, and then the restoration will be smoothed and polished. Initially, the dentist may want to trim the resin restoration with a surgical scalpel. Therefore, a scalpel handle and a surgical knife blade should be included in the setup. For the remaining finishing to be done, different finishing materials may be used depending on the nature of the restoration. Proximal resin restorations are finished with abrasive strips known as cuttlefish strips. They vary in width from one- sixteenth to three-sixteenths of an inch and are six inches in length. These are available in three grits: Fine, medium, and coarse. Cervical resin restorations are usually finished by using sandpaper disks mounted on a snap-head type mandrel. The disk mounted on a mandrel is used in conjunction with the handpieces. The snap-head mandrel is readily identified by its pyramid-shaped head over which the disc with a brass fitting will snap into place.

Alternative Finishing.

A restoration of one of the composite resins may be initially trimmed with a surgical knife and surgical knife blade. Other finishing may be done with some type of finishing bur or with a diamond cone or abrasive wheel that is used in conjunction with handpieces. White and green stones may also be used for this procedure. After using the stones, cuttlefish strips and fine sandpaper disks might be employed as a final finishing measure.

Tooth-colored composite fillings

Advantages:

- Aesthetics - the shade/color of the composites can be closely matched to the color of existing teeth; is particularly well suited for use in front teeth or visible parts of teeth

- Bonding to tooth structure - composite fillings actually chemically bond to tooth structure, providing further support to the tooth

- Versatility in uses - in addition to use as a filling material for decay, composite fillings can also be used to repair chipped, broken or worn teeth

- Tooth-sparing preparation - sometimes less tooth structure needs to be removed compared with amalgams when removing decay and preparing for the filling

Disadvantages:

- Lack of durability - composite fillings wear out sooner than amalgams (lasting at least 5 years compared with at least 10 to 15 for amalgams); in addition, they may not last as long as amalgams under the pressure of chewing and particularly if used as the filling material for large cavities

- Increased chair time - because of the process to apply the composite material, these fillings can take up to 20 minutes longer than amalgams to place

- Additional visits - if composites are used for inlays or onlays, more than one office visit may be required

- Chipping - depending on location, composite materials can chip off the tooth

- Expense - composite fillings can cost up to twice the cost of amalgams

In addition to tooth-colored, composite resin fillings, two other tooth-colored fillings exist--ceramics and glass ionomer.

#### Direct Restorative Dental Materials

| FACTORS | AMALGAM | COMPOSITES Direct and Indirect | GLASS IONOMERS | RESIN- IONOMERS |
| --- | --- | --- | --- | --- |
| General Description | A mixture of mercury and silver alloy powder that forms a hard solid metal filling. Self-hardening at mouth temperature. | A mixture of submicron glass filler and acrylic that forms a solid tooth-colored restoration. Self- or light-hardening at mouth temperature. | Self-hardening mixture of fluoride containing glass powder and organic acid that forms a solid tooth colored restoration able to release fluoride. | Self or light- hardening mixture of sub-micron glass filler with fluoride containing glass powder and acrylic resin that forms a solid tooth colored restoration able to release fluoride. |
| Principal Uses | Dental fillings and heavily loaded back tooth restorations. | Esthetic dental fillings and veneers. | Small non-load bearing fillings, cavity liners and cements for crowns and bridges. | Small non-load bearing fillings, cavity liners and cements for crowns and bridges. |
| Leakage and Recurrent Decay | Leakage is moderate, but recurrent decay is no more prevalent than other materials. | Leakage low when properly bonded to underlying tooth; recurrent decay depends on maintenance of the tooth-material bond. | Leakage is generally low; recurrent decay is comparable to other direct materials, fluoride release may be beneficial for patients at high risk for decay. | Leakage is low when properly bonded to the underlying tooth; recurrent decay is comparable to other direct materials, fluoride release may be beneficial for patients at high risk for decay. |
| Overall Durability | Good to excellent in large load-bearing restorations. | Good in small-to-moderate size restorations. | Moderate to good in non load-bearing restorations poor in load-bearing. | Moderate to good in non load-bearing restorations; poor in load-bearing. |
| Cavity Preparation Considerations | Requires removal of tooth structure for adequate retention and thickness of the filling. | Adhesive bonding permits removing less tooth structure. | Adhesive bonding permits removing less tooth structure. | Adhesive bonding permits removing less tooth structure. |
| Clinical Considerations | Tolerant to a wide range of clinical placement conditions, moderately tolerant to the presence of moisture during placement. | Must be placed in a well-controlled field of operation; very little tolerance to presence of moisture during placement. |  |  |
| Resistance to Wear | Highly resistant to wear. | Moderately resistant, but less so than amalgam. | High wear when placed on chewing surfaces. |  |
| Resistance to Fracture | Brittle, subject to chipping on filling edges, but good bulk strength in larger high- load restorations. | Moderate resistance to fracture in high-load restorations. | Low resistance to fracture. | Low to moderate resistance to fracture. |
| Biocompatibility | Well-tolerated with rare occurrences of allergenic response. |  |  |  |
| Post-Placement Sensitivity | Early sensitivity to hot and cold possible. | Occurrence of sensitivity highly dependent on ability to adequately bond the restoration to the underlying tooth. | Low. | Occurrence of sensitivity highly dependent on ability to adequately bond the restoration to the underlying tooth. |
| Esthetics | Silver or gray metallic color does not mimic tooth color. | Mimics natural tooth color and translucency, but can be subject to staining and discoloration over time. | Mimics natural tooth color, but lacks natural translucency of enamel. | Mimics natural tooth color, but lacks natural translucency of enamel. |
| Relative Cost to Patient | Generally lower; actual cost of fillings depends on their size. | Moderate; actual cost of fillings depends on their size and technique. | Moderate; actual cost of fillings depends on their size and technique. | Moderate; actual cost of fillings depends on their size and technique. |
| Average Number of Visits To Complete | One. | One for direct fillings; 2+ for indirect inlays, veneers and crowns. | One. | One. |

Literature.

1.Терапевтическая стоматология детского возраста. Хоменко Л.А., Чайковский Ю.Б., Савичук А.В., Савичук Н.О. и др.// К.:«Книга плюс» - 2013. – p. 267-345.

2.Ніколішин А.К.Терапевтична стоматологія. Том 1// Полтава: «Дивосвіт» - 2012. – p. 76-98.

3.Nikhil Marwah. Textbook of pediatric dentistry.//New Delhi: Jaypee Brothers Medical Publishers. 2011, p. 65-69.

4.Christian H.Splieth. Revolutions in pediatric dentistry //Quintessence Publishing Company, Incorporated: - 2011. – p.7 6-78.

5.David M. Sullivan. Manual of Pediatric dentistry //Lexi-Comp Incorporated,- 2012- p. 54-63.