Odesa National Medical University

Department of paediatric dentistry

METHODICAL RECOMMENDATIONS

for students

Academic discipline: “ Propaedeutics of pediatric dentistry”

Lesson № 7 “Materials for filling: cements and amalgams.

Physical and chemical properties of modern cements and amalgams.

Techniques of use. Filling of carious cavities  1 and 5 classes by Black in the temporary and permanent teeth in children”

Course 2. Faculty of Dentistry

Speciality.   221 “Dentistry”

«Затверджено»

На методичній нараді кафедри

стоматології дитячого віку

протокол № ___ від ______2021р.

Зав. кафедрою ________проф. О.В.Дєньга

Odessa   2021

Materials for filling: cements and amalgams.

Physical and chemical properties of modern cements and amalgams.

Techniques of use.Filling of carious cavities  1 and 5 class es by Black in the temporary and permanent teeth in children.

1. Concrete aims

To know classification of stomatological stopping materials.

To know classification, composition, basic physical and chemical properties, testimonies to application, technique of preparation and use of stomatological cements, including, ionomers.

To know the basic groups of materials for insulating and curative gaskets, them basic properties, testimony to application.

To know classification, composition, basic physical and chemical properties, testimonies to application and technique of the use of amalgam.

Able to stop stomatological cements, including ionomers, on phantoms carious cavities And and V of classes in temporal and permanent teeth with the unformed roots.

Able to prepare and lay on in carious cavities on phantoms insulating and curative gaskets.

Able to stop an amalgam on phantoms carious cavities And and V of classes in temporal and permanent teeth with the unformed roots.

2Base level of preparation

| Name of previous disciplines | Gained knowledge, abilities, skills |
| --- | --- |
| 1. Histology 2. Anatomy | To know the periods of development of temporal and permanent teeth. To know the histological structure of hard tissues of temporal and permanent teeth. To know the anatomic signs of different groups of temporal and permanent teeth. Able to determine group belonging of temporal and permanent teeth.. |

3. Organization of maintenance educational to the module

Classification of stomatological stopping materials : cements and amalgam.

2. Composition, basic physical and chemical properties, testimonies, is to application,

technique of preparation and use of different kinds stomatological cements: phosphatic, silicate and polycarbonates.

3. Composition, basic physical and chemical properties, testimonies, is to application           and technique of the use of amalgam.

4.Техніка stopping of carious cavities And and V of classes

by ionomer cements.

5. Technique of imposition of insulating gaskets with application zinc-

phosphatic and polycarboxilate cements: Zn-polycarboxilate and  ionomere.

6. A technique of imposition of curative gaskets is with application of fenol cements.

- Technique of stopping of carious cavities And and V of classes by an amalgam.

- Table of contents of educational material.

A dental restoration or dental filling is a dental restoration  used to restore the function, integrity and morphology of missing tooth structure. The structural loss typically results from caries or external trauma. It is also lost intentionally during tooth preparation to improve the aesthetic or the physical integrity of the intended restorative material.

A tooth preparation is the finished product of a tooth's structure prior to restoration with a dental restorative material, such as gold , amalgam, composite, porcelain or any number of other materials.

Glass ionomer cement

A glass ionomer cement (GIC) is one of a class of materials commonly used in dentistry as filling materials and luting cements. These materials are based on the reaction of silicate glass powder and polyalkeonic acid. These tooth-coloured materials were introduced in 1972 for use as restorative materials for anterior teeth (particularly for eroded areas, Class III and V cavities).

As they bond chemically to dental hard tissues and release fluoride for a relatively long period modern day applications of GICs have expanded. The desirable properties of glass ionomer cements make them useful materials in the restoration of carious lesions in low-stress areas such as smooth-surface and small anterior proximal cavities in primary teeth. Results from clinical studies also support the use of conventional glass ionomer restorations in primary molars. They need not be put in layer by layer, like in composite fillings.

Glass ionomers are translucent, tooth-colored materials made of a mixture of acrylic acids and fine glass powders that are used to fill cavities, particularly those on the root surfaces of teeth. Glass ionomers can release a small amount of fluoride that may be beneficial for patients who are at high risk for decay. When the dentist prepares the tooth for a glass ionomer, less tooth structure can be removed; this may result in a smaller filling than that of an amalgam.

Glass ionomers are primarily used in areas not subject to heavy chewing pressure. Because they have a low resistance to fracture, glass ionomers are mostly used in small non-load bearing fillings (those between the teeth) or on the roots of teeth.

Resin ionomers also are made from glass filler with acrylic acids and acrylic resin. They also are used for very small, non-load bearing fillings (between the teeth), on the root surfaces of teeth, and they have low to moderate resistance to fracture.

Ionomers experience high wear when placed on chewing surfaces. Both glass and resin ionomers mimic natural tooth color but lack the natural translucency of enamel. Both types are well tolerated by patients with only rare occurrences of allergic response.

Amalgam

Historically, dental amalgam is the most popular restorative material . Its main advantage is that it is relatively economical and simple to use . However, whilst amalgam possess excellent physical properties, it is not adhesive and therefore cavity design needs to include some form  of mechanical retention. Possibly the biggest problem associated with its use in the recent upsurge in public option concerning its safety. In many countries the use of amalgam in children ‘s teeth has been restricted . The rational for these restrictions is based upon environmental concerns rather than concerns over amalgam toxicity. Nevertheless, the dental profession may be forced into using alternatives to amalgam by a combination of public option and legislation.

Advantages  : simple , quick, cheap, technique insensitive, durable.

Disadvantage : not adhesive, requires mechanical retention in cavity, environmental and occupational hazards, public concern.

The use of dental amalgam to restore primary molars is common and supported by evidence from clinical trials. Clinical studies, evaluating the durability of dental amalgam in primary molars, have laid down the benchmarks against which other restorations should be judged.

The success rate for class 11 amalgam restoration in primary molars has been reported as between 70% and 80%.

Indications

Amalgam may be useful in children who are at moderate caries risk or who are not totally cooperative , i.e. where moisture control is problem .

There is limited indication  for the use of amalgam in class 1 cavites in children.

The use of amalgam is decreasing , given the increasing concern and wishes from perents to avoid its use.

Method for interproximal (class 11) amalgam restoration.

Use local anaesthesia and rubber –dam isolation.

Use a small round or pear-shaped  diamond bur in a high- speed handpiece to gain acces to the caries. The occlusal outline should not extend into all the fissures but needs to incorporate a small isthmus and a dovetail for retention. AMALGAM RESTORATIONS WITH CEMENT BASE

a. General. Preparing and restoring teeth with silver amalgam is the dental treatment procedure performed most frequently. The properties of silver amalgam are determined largely by how it is handled. Optimum properties can be achieved only through careful attention to details in its preparation and manipulation. Since the dental assistant normally is responsible for the measurement, preparation, and initial handling of the material, the manner in which he carries out these procedures can determine the success of the restoration. In addition, the manner in which he assists the dentist in the performance of other steps of the restorative operation influences the quality of the results.

b. Instrument and Material Setup. The instruments and materials should not be introduced into the working area until just before they are needed. Instruments used for preceding steps and no longer needed should be removed from the working area. A typical setup for a Class II amalgam restoration includes the instruments and equipment shown in figure 2-29. Class I restorations normally will not require the matrix material.

c. Preparing and Placement of Cement Base.

(1) General. It is common practice to insert a low thermal conducting cement material as a base in deep portions of cavities underlying metallic restorations to insulate the pulp against thermal and electrical shock and pressures induced during placement of the restorations. Zinc phosphate cement is the material most used for this purpose.

(2) Assisting procedures. When the dentist is finishing the cavity preparation, he will direct the dental assistant to prepare the base. The dental assistant manipulates the material in accordance with the manufacturer's directions and the general techniques discussed in a previous subcourse. A thick mix is normally used for this purpose. When the dental assistant has completed the mix to the desired consistency, it is presented to the dentist. Usually, the mix is scraped from the spatula onto the center of one edge of the glass slab. Some dentists may want the glass slab placed on the bracket table, while others may want it held by the specialist while the dentist takes the amount of material required. Some excess powder should remain for the dentist's use in placing the base. Upon completion of the placement of the base, the dental assistant should remove the slab and spatula from the operative area. If zinc phosphate is used as a base, we will of course need a glass slab (which should have a "Z" or "ZP" etched on the side) with a matched set of zinc phosphate powder and liquid. There are several other base materials, which may be used and most of these will be mixed on paper or parchment mixing pads. We will also need a stainless steel spatula in mixing all of the base materials. To carry and pack the cement into the preparation requires the use of one of several cement pluggers available to the dentist. One of the more commonly used pluggers is the Ladmore plugger number 3, which has teardrop shaped working ends on both ends of the instrument. The Woodson pluggers number 1, number 2, and number 3 may also be used. Both nibs of the Woodson number 1 are flat, one in the same plane of the shank and the other at a slight angle to the shank. The Woodson number 2 has a cylinder-shaped plugger on one end and a paddle-shaped nib on the other. A Woodson number 3 has nibs similar to the Woodson number 2 except that the cylinder-shaped nib is larger. Many dentists will prefer to use a much smaller base instrument we call the "Dycal instrument." This instrument is furnished by certain manufacturers with their base materials. It is much shorter and smaller than the others we have discussed and has a beaded end to the nib.

e. Preparing Amalgam. The dental assistant then prepares the amalgam in accordance with the manufacturer's instructions and general techniques discussed in a previous lesson. The manner in which the assistant handles the dental amalgam will have much to do with the success of the resulting restoration. Correct trituration time and avoidance of moisture contamination are important steps in producing the material with the best properties.

f. Filling the Cavity. In an amalgam restoration, the amalgam will be prepared in an amalgamator, and the dentist can place the amalgam into the preparation with the amalgam carrier. This instrument has a barrel type nib that is used to pick up and transfer the amalgam from the squeezed cloth to the mouth.

CAUTION: Remember never to touch the amalgam with your hands.

Once it is placed in the restoration, the amalgam must be condensed. This is done with amalgam pluggers. The two pluggers that will be used are the Black's number 1 and number 2. They both have round-shaped plugger ends with the end of the number 2 somewhat larger than the number 1. The alternate pluggers take different shapes on the working ends. The dental assistant loads the amalgam carrier with the amalgam and places it in the dentist's operating hand in the position in which he will carry it to the tooth. The dental assistant then picks up the first amalgam plugger in his right hand. When the dentist is ready for the plugger, the dental assistant takes the amalgam carrier from him and replaces it with the plugger. While the dentist is condensing the first segment of amalgam, the dental assistant loads the carrier with the next segment. In this way, the cavity is filled segment by segment, the dental assistant alternately passing the loaded amalgam carrier and appropriate instruments to the hand of the dentist. When the cavity is sufficiently filled, the dental assistant selects the appropriate carving instruments and hands them one at a time to the dentist as needed. The exchange of instruments between the hands of the assistant and operator is done to keep the dentist's hands close to the patient's mouth and to foster rapid and smooth accomplishment of the operative procedure. When the matrix material has been removed from the mouth, the dental assistant should also be prepared to rinse the patient's mouth as necessary during and after final carving procedures.

g. Finishing and Polishing Amalgam Restorations

(1) Amalgam covers. Finally, the dentist is ready to finish the restoration. In this step, he will complete the procedure so that patient is able to function normally. In placing the amalgam, the dentist will overfill the preparation during the condensation phase to obtain sufficient bulk of material to carve the amalgam down to the original contour of the tooth. He will use amalgam carvers to contour the partially crystallized amalgam. He may employ the Hollenback number 3, the cleoid number 92, and the discoid number 89. The Hollenback number 3 has two grain-shaped blades. The cleoid carver has only one blade, a concave pointed oval that resembles a claw. In fact, you will find that in the Medical Supply Catalog this instrument is listed as a claw excavator. The discoid amalgam carver has a single blade that is round or disc-shaped (from which its name comes, discoid).

(2) Articulating paper. The final item is articulating paper. It closely resembles blue carbon paper and is issued in a roll or package form. Desired lengths are cut from the roll or selected from the package, and the patient is instructed to bite down normally with the strip of articulating paper over the occlusal surfaces of the teeth. Any high spots in the patient's occlusion will be detected by noting blue spots on the teeth. The dentist may have a patient return for final finishing and polishing of the amalgam restoration 24 or more hours after its insertion. This is done to eliminate small excesses of amalgam that may have been left overhanging cavity margins, to refine occlusal contours of the restoration, and to develop a smooth, shiny surface that will resist contamination and formation of surface oxides.

(3) Materials. Finishing and polishing is done with fine polishing disks and strips, green stones, finishing burs, chalk, and other fine polishing agents. An old contra-angle hand piece is operated at slow speed along with "wet" solutions (mixtures) of polishing materials to minimize heat production. Heat produced during the polishing could weaken the surface of the amalgam. Rubber polishing cups and polishing brushes are commonly used to apply the polishing materials.

NOTE: Figure 2-31 outlines steps of procedure for the dental assistant and the dentist, when preparing amalgam restorations with a cement base.

Additional information:

Amalgam, produced by mixing mercury and other metals, is still the most commonly used filling material. Some people have expressed concern about amalgam because of its alleged mercury content. In fact, amalgam is composed mostly of complex compounds where the mercury is bound chemically to the other ingredients. Although mercury by itself is classified as a toxic material, the mercury in amalgam is chemically bound to other metals to make it stable and therefore safe for use in dental applications. In fact, amalgam is the most thoroughly studied and tested restorative material now used. Compared to the rest, it is durable, easy to use, and inexpensive. The safety and effectiveness of amalgam have been reviewed by major U.S. and international scientific and health bodies, including the American Dental Association; the National Institutes of Health; the U.S. Public Health Service; the Centers for Disease Control and Prevention; the Food and Drug Administration; and the World Health Organization. All have concluded that amalgam is a safe and effective material for restoring teeth.

The charts below are reproduced with the kind permission of the American Dental Association, which developed them to help dentists explain the relative advantages and disadvantages of the materials used in fillings, crowns, bridges and inlays. They provide a simple overview of the subject based on the current dental literature and are not intended to be comprehensive. The attributes of a particular restorative material can vary from case to case depending on a number of factors.

Silver-fillings (Amalgams)/Advantages:

Durability - lasts at least 10 to 15 years and usually outlasts composite fillings.

Strength - can withstand chewing forces

Expense - is less expensive than composite fillings

Disadvantages:Poor aesthetics - fillings don't match the color of your natural teeth

Destruction of more tooth structure - healthy parts of the tooth must often be removed to make a space large enough to hold the amalgam filling

Discoloration - amalgam fillings can create a grayish hue to the surrounding tooth structure

Cracks and fractures - although all teeth expand and contract in the presence of hot and cold liquids, which ultimately can cause the tooth to crack or fracture, amalgam material - in comparison with other filling materials-may experience a wider degree of expansion and contraction and lead to a higher incidence of cracks and fractures

Allergic reactions - a small percentage of people, approximately 1%, are allergic to the mercury present in amalgam restorations

#### Direct Restorative Dental Materials

| FACTORS | AMALGAM | COMPOSITES Direct and Indirect | GLASS IONOMERS | RESIN- IONOMERS |
| --- | --- | --- | --- | --- |
| General Description | A mixture of mercury and silver alloy powder that forms a hard solid metal filling. Self-hardening at mouth temperature. | A mixture of submicron glass filler and acrylic that forms a solid tooth-colored restoration. Self- or light-hardening at mouth temperature. | Self-hardening mixture of fluoride containing glass powder and organic acid that forms a solid tooth colored restoration able to release fluoride. | Self or light- hardening mixture of sub-micron glass filler with fluoride containing glass powder and acrylic resin that forms a solid tooth colored restoration able to release fluoride. |
| Principal Uses | Dental fillings and heavily loaded back tooth restorations. | Esthetic dental fillings and veneers. | Small non-load bearing fillings, cavity liners and cements for crowns and bridges. | Small non-load bearing fillings, cavity liners and cements for crowns and bridges. |
| Leakage and Recurrent Decay | Leakage is moderate, but recurrent decay is no more prevalent than other materials. | Leakage low when properly bonded to underlying tooth; recurrent decay depends on maintenance of the tooth-material bond. | Leakage is generally low; recurrent decay is comparable to other direct materials, fluoride release may be beneficial for patients at high risk for decay. | Leakage is low when properly bonded to the underlying tooth; recurrent decay is comparable to other direct materials, fluoride release may be beneficial for patients at high risk for decay. |
| Overall Durability | Good to excellent in large load-bearing restorations. | Good in small-to-moderate size restorations. | Moderate to good in non load-bearing restorations poor in load-bearing. | Moderate to good in non load-bearing restorations; poor in load-bearing. |
| Cavity Preparation Considerations | Requires removal of tooth structure for adequate retention and thickness of the filling. | Adhesive bonding permits removing less tooth structure. | Adhesive bonding permits removing less tooth structure. | Adhesive bonding permits removing less tooth structure. |
| Clinical Considerations | Tolerant to a wide range of clinical placement conditions, moderately tolerant to the presence of moisture during placement. | Must be placed in a well-controlled field of operation; very little tolerance to presence of moisture during placement. |  |  |
| Resistance to Wear | Highly resistant to wear. | Moderately resistant, but less so than amalgam. | High wear when placed on chewing surfaces. |  |
| Resistance to Fracture | Brittle, subject to chipping on filling edges, but good bulk strength in larger high- load restorations. | Moderate resistance to fracture in high-load restorations. | Low resistance to fracture. | Low to moderate resistance to fracture. |
| Biocompatibility | Well-tolerated with rare occurrences of allergenic response. |  |  |  |
| Post-Placement Sensitivity | Early sensitivity to hot and cold possible. | Occurrence of sensitivity highly dependent on ability to adequately bond the restoration to the underlying tooth. | Low. | Occurrence of sensitivity highly dependent on ability to adequately bond the restoration to the underlying tooth. |
| Esthetics | Silver or gray metallic color does not mimic tooth color. | Mimics natural tooth color and translucency, but can be subject to staining and discoloration over time. | Mimics natural tooth color, but lacks natural translucency of enamel. | Mimics natural tooth color, but lacks natural translucency of enamel. |
| Relative Cost to Patient | Generally lower; actual cost of fillings depends on their size. | Moderate; actual cost of fillings depends on their size and technique. | Moderate; actual cost of fillings depends on their size and technique. | Moderate; actual cost of fillings depends on their size and technique. |
| Average Number of Visits To Complete | One. | One for direct fillings; 2+ for indirect inlays, veneers and crowns. | One. | One. |

Literature.

1.Терапевтическая стоматология детского возраста. Хоменко Л.А., Чайковский Ю.Б., Савичук А.В., Савичук Н.О. и др.// К.:«Книга плюс» - 2013. – p. 267-345.

2.Ніколішин А.К.Терапевтична стоматологія. Том 1// Полтава: «Дивосвіт» - 2012. – p. 76-98.

3.Nikhil Marwah. Textbook of pediatric dentistry.//New Delhi: Jaypee Brothers Medical Publishers. 2011, p. 65-69.

4.Christian H.Splieth. Revolutions in pediatric dentistry //Quintessence Publishing Company, Incorporated: - 2011. – p.7 6-78.

5.David M. Sullivan. Manual of Pediatric dentistry //Lexi-Comp Incorporated,- 2012- p. 54-63.