ODESSA NATIONAL MEDICAL UNIVERSITY

Department of Biophysics, Informatics and Medical Devices

Information

for

First year students

Taking the course of

Biological physics with physical methods of analysis

Specialty: 226 «Pharmacy, industrial pharmacy»

IWS 04 2h

Continuum mechanics

Composed by:

As. Prof. P.G. Zhumatii

Approved

at the methodical meeting of the Department

"29" _August_ 2023,    Protocol No. _1_

Head of Department, Prof. 		Godlevsky L.S.

ODESSA – 2023

IWS 04 2h Continuum mechanics.

Deformation is the change in the distances between material points, which leads to changes in shape and/or size of the body.

All real materials undergo some deformation under the influence of forces:

- deformation consisting only of volume change is known as dilation;

- deformation, involving change of shape at constant volume, is known as distortion.

A material that can undergo only distortion and not dilatation is called incompressible; dense rubber comes fairly close to being such a material.

Schematic of various loading modes:

A tensile force applied to a bar produces an elongation.

The applied force/area is called the stress  σ = Fapplied/A.

- When L = L0 the material is relaxed.

- When there is a positive Fapplied, the material is under tension and L > L0.

- If there is a negative Fapplied, the material is under compression and L < L0.

Suppose that a force pulling on a bar of initial length  L0  stretches it by an amount

ΔL = L ‒ L0. The elongation per unit length,  ΔL/L,  is independent of the length of the bar. This quantity is known as longitudinal strain and is usually denoted  ε, that is,

Any device in which the application of a load produces a displacement that increases with the load is called a spring.

The ratio between load and displacement is called the spring constant, denoted simply  k. If  F  denotes the force and  x  the displacement of the spring, then

F = kx .

The linear spring is the prototype of a behavior in bodies called linear elasticity.

The linear elasticity of the material in uniaxial loading is given by a linear relation between σ and ε,

σ = Eε .

This equation  represents the uniaxial Hooke’s law, and the coefficient E is known as the modulus of elasticity, or Young’s modulus of the material. The elastic modulus  is a measure of a material’s resistance to distortion by a tensile or compressive load.

As with the load-displacement relation in springs, most solids exhibit a linear uniaxial stress–strain relation only for a certain range of strains. This range depends on the material and may vary from approximately 0.1% for metals to more than 100% for rubber.

When shear forces are applied to a rectangular block, then the result will be a distortion. The applied load is parallel to the area supporting it (shear stress, τ ).

The deformation of the rectangular block is evidenced by the fact that it is no longer rectangular. The change  γ  from a right angle may be used as the measure of shear strain.

A relation   between the shear stress  τ  and the shear strain  γ  is

τ = Gγ ,

where  G is known as the shear modulus.

The bulk modulus (K, units of Pascals) quantifies the variation in volume (dV) of a

material when the pressure is changed (dp). It is defined through the equation

The negative sign allows positive compressibilities to describe the typical case where an increase in pressure causes a decrease in volume.

We know from experience that when a slender body is pulled along its axis, the material contracts in the directions perpendicular to this axis.

If the longitudinal strain along the axis is tensile and equal to  εlong > 0, and if the contraction along transverse direction is represented by the lateral strain  εlat < 0, then

is a material parameter known as the Poisson’s ratio.

This Poisson’s ratio characterizes the severity of the lateral contraction experienced by the material when subjected to uniaxial elongation.

For an isotropic elastic material the bulk modulus K, Young’s modulus E, shear modulus  G  and Poisson ratio  ν  are interrelated by two simple relationships,

Stress–strain diagram

To this point, we have limited the discussion to small strains << 1, such that all imposed deformations are completely recoverable. This is the elastic response region.

What happens at larger deformations, however, is dependent to some extent on the

type of material under consideration. Beyond the elastic region, we enter a realm of nonrecoverable mechanical response termed permanent deformation.

a                                                                     b

Figure a  shows a realistic stress–strain relation:

- There is elastic Hookean behavior up to the point P, the proportional limit. The slope up

to this stress is constant, the Young’s modulus  E . The higher the  E , the stiffer the material.

- At higher stresses, the stress–strain relation is nonlinear. Up to the elastic limit, denoted

by  EL, the object returns to its initial length when the stress is removed.

- For stresses beyond the elastic limit, there is permanent or plastic deformation and the

length and shape of the object are different after the stress is removed.

The yield limit, denoted by YP, is at a stress somewhat higher than the elastic limit;

above it much elongation can occur without much increase in the load.

The yield point is usually estimated by the intersection of the stress–strain curve with a

line parallel to the linear part of the stress–strain curve, but with an intercept set at a strain of  0.2% (or 0.002). The yield point occurs at the yield stress (or strength), YS.

- For tension, the material remains intact for larger stresses until the ultimate tensile stress

(UTS), which is also called the tensile strength (TS).  Application of this stress leads to fracture at point F, which occurs at a strain called the ultimate strain or the ultimate percent elongation (UPE).

- The final point F represents the rupture point or fracture point, of the material. The

stress at point  F is called the fracture strength  σf . It is simply the point at which the material physically separates into two or more pieces.

In Figure a, the actual type of stress being plotted is called the engineering stress  σeng = F/A0.  It is the force divided by the initial area.

Past the UTS, the  σeng  decreases, the material becomes narrower as it is pulled apart. The actual area  A  becomes progressively smaller than this initial area, which is called “necking”. The true stress  σtrue = F/A  increases after the UTS, due to this necking.

These stress–strain relations look qualitatively different for ceramics, metals, and elastomers because of the very different microscopic structures of these types of materials (Figure a).

a                                                        b

Ceramics have a linear stress–strain relation with large slope E . The fracture point appears only a little into the nonlinear elastic regime, and for smaller values of strain ε <0.1.

Metals have a smaller E , a larger nonelastic and plastic regime, and a larger UPE ~ 50 (in %).

Elastomers (rubber, polymers) distort greatly even with small stresses because in this regime long, tangled chain molecules are straightened out at low stress in this toe region (the region of positive curvature at low strain). The stress–strain curve is not linear. It takes much larger stresses to increase strain further after all of the chains have been straightened, because now bonds must be stretched. These materials have a very large UPE, typically >1.

Typical stress–strain curves for structural materials in the body under tension are shown in Figure b:

- To first order, bones, teeth, and nails, all hard materials, have similar stress–strain curves

that are ceramic-like.

- Tendons, cartilage, resting muscle, skin, arteries, and intestines all have more elastomer-

like properties because they have much more collagen; they are non-Hookean materials.

Time-Dependent Deviations from Elastic Behavior: Viscoelasticity

For all the mechanical behaviors considered to this point, it has been assumed that when a stress is applied, the strain response is instantaneous. For many important biomaterials, including polymers and tissues, this is not a valid assumption.

The responses of most materials depend on time and on history, to some degree. This very important type of mechanical behavior is called viscoelasticity.

Viscoelasticity is the response of a material to an applied stress that has both a viscous and an elastic component.

In addition to a recoverable elastic response to an applied force, materials can undergo permanent deformation at high strains for a considerable time even though the load is constant. This continuous, time-dependent extension under constant load is called creep.

Similarly, if the material is extended in a tensile machine to a fixed elongation and held constant while the load is monitored, the load drops continuously with time. The continuous drop in load at constant extension is called stress relaxation.

Both these responses are the result of viscous flow in the material. The mechanical analog of viscous flow is a dashpot or cylinder and piston. Any small force is enough to keep the piston moving. If the load is increased, the rate of displacement will increase.

Perfectly harmonic elastic behavior is modeled by a spring, with

F(t) = kx(t),

where  F  is now the applied force and  x  is the response, which is the displacement of the end of the spring, k  is the spring constant. The force and displacement depend on the current state at the current time  t  and are independent of history.

Perfectly viscous behavior is modeled by a dashpot, with

F(t) = cv(t),

where the response depends on the speed   v(t),  c  is a damping constant that describes damping due to viscosity. This characterization is often used to describe friction and other types of energy relaxation and dissipation.

An idealized dashpot is a piston moving in a cylinder, impeded by its movement in a viscous fluid. The displacement of the piston in the dashpot depends on its history!

Simple Viscoelastic Models

Biological liquids and solids are usually viscoelastic, and this includes tendons, ligaments, cartilage, bone, and mucous. Three models are commonly used to describe viscoelastic materials. Each combines these idealized springs and dashpots in different ways.

- A Maxwell body is a dashpot and spring in series (a).

a                                                b                               c

In the creep experiment (b), there is an immediate spring-like response. Then the

deformation increases linearly in time, as for the dashpot. When the force is removed, the deformation immediately decreases to the value determined by the spring component, and there is no more creep due to the dashpot.

In the stress relaxation experiment (c), there is an immediate force response due to the spring element, but this response decreases in an exponential manner, as  exp(−t/τ ), due to the dashpot. The parameter  τ = c/k  is called a time constant; it has the units of seconds.

2.   A Voigt body is a dashpot and spring in parallel (a).

a                                                b                               c

In the creep experiments (b), there is an exponential increase in creep, as

1 − exp(−t/τ ), due to the dashpot,  where again  τ = c/k. If the force is removed, this

deformation decays to zero exponentially as exp(−t/τ ).

This is qualitatively different from the predictions of the Maxwell model.

In the stress relaxation experiments (c), there is an immediate and temporary

increase in force, as seen for the dashpot alone, and then the response is the constant value expected from the spring alone.

3.  A Kelvin body is a dashpot and spring in series, which are in parallel with another spring (a). The Kelvin model is also called the standard linear model.

a                                                b                               c

The time constants  τε  = c/k1 ,  τσ = c(1/k1 + 1/k2).

In the creep experiments (b), there is an immediate increase due to the  k1 spring

and then due to the dashpot an exponential increase in creep, as   1− exp(−t/τσ).

When the force is removed, this strain decays to zero exponentially as  exp(−t/τσ).

In the stress relaxation experiments (c), there is an immediate finite increase in

force, and then the response relaxes as  exp(−t/τε)  to a constant value.

The Maxwell and Voigt models are special cases of the Kelvin model, and consequently, the Kelvin model exhibits characteristic features of both simpler models. Why do not we always use the Kelvin model? Sometimes the use of the Kelvin model makes the analysis complex. More complex materials models consist of combinations of Kelvin models.

Hydro and hemodynamics

A fluid is defined as a substance that deforms continuously under application of a shearing stress, regardless of how small the stress is.

To study the behavior of fluids, it is useful to define a number of important fluid  properties, which include density and viscosity.

Density is defined as the mass per unit volume of a substance and is denoted by the Greek character ρ (rho). The SI units for  ρ  are kg/m3.

Two fluids with identical densities can flow quite differently when subjected to the same forces. The additional property that determines the difference in behavior is viscosity.

Shear stress and rate of shearing strain

To understand viscosity, let us begin by imagining a fluid between two parallel plates which are infinite in width and length.

The bottom plate A is a fixed plate. The upper plate B is a moveable plate, suspended on the fluid between the two plates. The distance between the two plates is h. A force  F  is applied to the plate B causing it to move along at a velocity VB  with respect to the plate A.

The shear stress  τ  in this case may be represented by

where  A - plate area.

Let the distance from the fixed plate to some arbitrary point above the plate be  y.

The velocity  V of the fluid between the plates is a function of the distance y:   V = V(y). Then, for small  dV  and  dy

dV/dy = γ.

The first derivative of the shearing strain with respect to time is known as shear rate  γ. The shear rate has the units of  1/s.

The shear stress  τ  on a fluid is related to the shear rate  γ. A way to visualize this relationship is by making a plot of shearing stress as a function of the shear rate.

The material property that is represented by the slope of the stress–shear rate curve is known as dynamic viscosity μ (mu). The SI units for dynamic viscosity are  Pa∙s.

Kinematic viscosity (SI units are  m2/s) is another fluid property that has been used to characterize flow. Kinematic viscosity ν can be defined by the equation:

For common fluids like oil, water, and air, viscosity does not vary with shear rate. Fluids with constant viscosity are known as Newtonian fluids. For Newtonian fluids

where  τ - shear stress,  μ – viscosity, γ - shear rate.

For non-Newtonian fluids, shear stress and shear rate are not linearly related and the slope of the shear stress/shear rate curve is not constant. However, we can define the apparent viscosity as the instantaneous slope of the shear stress/shear rate curve.

Shear thickening fluids are non-Newtonian fluids whose apparent viscosity increases when the shear rate increases.

Quicksand is a good example of a shear thickening fluid. If one tries to move slowly in quicksand, then the viscosity is low and the movement is relatively easy. If motion is quick, then the viscosity increases and the movement is difficult.

Shear thinning fluids are non-Newtonian fluids whose apparent viscosity decreases as shear rate increases. At low shear rates, blood is also a shear thinning fluid.

A Bingham plastic is neither a fluid nor a solid. A Bingham plastic can withstand a finite shear load and flow like a fluid when that shear stress is exceeded. For Bingham plastic, shear stress and rate of shearing strain may be related by the Shvedov-Bingham equation:

τ = τ0 + μγ ,

where  τ0  is the yield stress.

Toothpaste and mayonnaise are examples of Bingham plastics. Blood is also a Bingham plastic and behaves as a solid at shear rates very close to zero.

The Casson fluid (Casson, 1959), was proposed as a useful empirical model for blood

τ1∕2 = τ01∕2 + (μγ)1∕2 ,

where  τ0  is the blood yield stress.

Fluid dynamics

Fluid dynamics is dealing with liquids and gases in motion. It offers a systematic structure that embraces laws, derived from measurement, used to solve practical problems.

All fluids are compressible to some extent. However, in many situations the changes in pressure are sufficiently small that the changes in density are negligible. In this case the flow can be modeled as an incompressible flow and under circumstances where the mass inside the control volume does not change the continuity equation can be written in form:

where  Q  is the volume flow rate (SI units m3/s) going into and out of the control volume.

Laminar flow is highly organized flow along streamlines.

As velocity increases, flow can become disorganized and chaotic with a random 3-D motion superimposed on the average flow velocity. This is known as turbulent flow.

To predict the transition between laminar and turbulent flows helps us the Reynolds number - a dimensionless parameter named after Reynolds. The number is defined as

where  ρ  - fluid density in kg/m3,  D - pipe diameter in m, μ - fluid viscosity in Pa∙s,  V -   average fluid velocity in m/s across the pipe cross section.

- Laminar flow occurs in flow environments where  Re < 2000.

- Turbulent flow is present in circumstances under which  Re > 4000.

- The range of  2000 < Re < 4000  is known as the transition range.

Physically, the Reynolds number represents the ratio of inertial forces to viscous forces.

The Reynolds number is also useful for predicting entrance length XE  for fully developed flow in pipe.

The ratio of entrance length to pipe diameter for laminar pipe flow is given asngth

.

Consider the following example: If  Re = 300, then  XE = 18 D, and an entrance length equal to 18 pipe diameters is required for fully developed flow.

Although most blood flow in humans is laminar, having a Re of  300 or less, it is possible for turbulence to occur at very high flow rates in the descending aorta, for example, in highly conditioned athletes. Turbulence is also common in pathological conditions such as heart murmurs and stenotic heart valves.

Velocity as a function of radius

The solution of a fluid dynamics problem involves calculation of various properties of the fluid, such as velocity, pressure, density, as functions of space and time.

This law describes steady, laminar, incompressible, and viscous flow of a Newtonian fluid in a rigid, cylindrical tube of constant cross section.

Consider a cylinder of fluid in a region of fully developed flow and sum the forces acting on that cylinder.

Recall, from the definition of viscosity, that the shear stress is related to the shear rate:

If we solve these equations together, the velocity becomes

.

Note that dP/dx have a negative value; as pressure drops, that would give a positive velocity. This is consistent with the definition  of positive  x  as a value to the right, or downstream.

Note also that the maximum velocity will occur on the centerline.

Now it is possible to find the total flow passing through the tube. This yields the expression - Hagen-Poiseuille law:

.

Hagen-Poiseuille law can be successfully applied to blood flow in capillaries and veins, to air flow in lung alveoli, for the measurement of viscosity.

Viscosity Measurement

There are several methods of measurement of viscosity. Each of the various methods has its own advantages and disadvantages.

In 1851, Stokes derived an expression, known as Stokes' law, for the frictional force exerted on spherical objects in a continuous viscous fluid:

,

where   Fd is the frictional force,  μ is the fluid's dynamic viscosity,  R is the radius of the spherical object, and  V is the particle's velocity.

Stokes's law is the basis of the falling-sphere viscometer, in which the fluid is stationary in a vertical glass tube. A sphere of known size and density is allowed to descend through the liquid. When frictional force combined with the buoyant force exactly balance the gravitational force, it reaches terminal velocity, which can be measured by the time it takes to pass two marks on the tube.

The resulting terminal velocity is given by:

where  g is the gravitational acceleration (m/s2),  ρp is the mass density of the particles (kg/m3), and ρf is the mass density of the fluid (kg/m3).

Knowing the terminal velocity, the size and density of the sphere, and the density of the liquid, Stokes' law can be used to calculate the viscosity of the fluid.

Hemodynamics

The circulatory system is a connected series of tubes, which includes the heart, the arteries, the microcirculation, and the veins.

The heart is the driver of the circulatory system generating cardiac output (CO) by rhythmically contracting and relaxing. This creates changes in regional pressures, and, combined with a complex valvular system in the heart and the veins, ensures that the blood moves around the circulatory system in one direction.

In order to investigate complex blood flow phenomena, electrical analogs, which result in linear differential equations, were developed. In these models the vessel resistance to blood flow is represented by a resistor  R, the tube compliance by a capacitor  C, and blood inertia by an inductance L.

Assuming that blood flow  Q  and pressure  P are analogous to the electrical current I and voltage  U, respectively, blood flow through a compliant vessel (e.g., artery or vein) may be represented by an electrical scheme:

For a system of vessels attached in series (or small units of a nonuniform vessel) a more complicated scheme, composed of a series of compartments whose characteristics are represented by  Ri, Ci, and  Li, is used. This compartmental approach allowed for computer simulations of complex arterial circuits with clinical applications.