ОДЕСЬКИЙ НАЦІОНАЛЬНИЙ МЕДИЧНИЙ УНІВЕРСИТЕТ

Кафедра стоматології дитячого віку

Lecture

Introduction to restorative materials

III semester, 2 course

Лекцію обговорено на
методичній нараді кафедри

"02"    вересня      2016  р.

Протокол №

Зав. кафедрою стоматології

дитячого віку,

професор	Дєньга О.В.

Одеса 2016 р.

Lecture

Introduction to restorative materials

1. Actuality of the topic. Explanation of the topic. Dentistry is the branch of medicine that is involved in the study, diagnosis, prevention, and treatment of diseases, disorders and conditions of the oral cavity, the maxillofacial area and the adjacent and associated structures, and their impact on the human body. To the layman, dentistry tends to be perceived as being focused primarily on human teeth, though it is not limited strictly to this. Dentistry is widely considered necessary for complete overall health.

The stomatology of children's age is allocated among all stomatological disciplines, any physiological and pathological processes in child organism proceed immediately and all protective reactions are unstable (neuroendocrinal system, immunal status, etc. are not formated);

In connection with features of formation and development of a child organism at various stages (growth of a skeleton, muscles, a fiber lack, formation of bodies and systems) it’s necessary to use various approaches to prophylaxis and treatment (it’s especially important in orthodontics);

The pathological processes proceeding in the    child organism, as a rule, are reversible unlike an adults organism (caries, parodontic diseases);

2. The purpose of the lecture.

А. Educational: For the children's dentist the most important are general medical knowledge, as a rule dentist    first sees system diseases - especially important are diseases of blood, infringement of a bone metabolism, gastrointestinal tract, a pathology of kidneys, endocrinic and other pathologys.

3. Plan and the structure of the lecture.

| № | Basic stages and its content | Purpose in conditions of abstraction | Type of the lecture equipment | Time distribution |
| --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 4 | 5 |
| 1. 2. 3. | Preparatory stage - Definition of the educational purpose - Ensuring of the positive motivation Basic stage - Introduction to restorative materials -classification of filling materials -advantages and disadvantages of modern filling materials Final stage - summary of the lecture - answers the lectures - tusks for the self-preparation of the students | 3 2 3 | 4табл.(мульт.) 5 рис.(мульт.) | 2 3 38 15 25 2 |

4. Content of the lecture:

- structural-logical scheme of the lecture;

- text of the lecture

A dental restoration or dental filling is a dental restorative material used to restore the function, integrity and morphology of missing tooth structure. The structural loss typically results from caries or external trauma. It is also lost intentionally during tooth preparation to improve the aesthetics or the physical integrity of the intended restorative material. Dental restoration also refers to the replacement of missing tooth structure which is supported by dental implants.

Dental restorations can be divided into two broad types: direct restorations and indirect restorations. All dental restorations can be further classified by their location and size.

- filling material must be biologically compatible with human organism;

- filling material must not contain any substances that may cause an allergic reaction;

- filling material must not be poisonous;

- filling material must have adhesion to dental tissues;

- filling material must be hard enough to handle the strain of biting, chewing and grinding;

resistance to wear and to fracture is important;

- filling material must not    collapse in aggressive environment of oral cavity;

-harden and save its properties in wet environment;

- filling material must not change the colour of dental tissues;

- filling material must have modulus of flexibility and coefficient of thermal expansion close to dental tissues;

- filling material must be aesthetically.

Classification:

Bases and Liners

Cavity varnishes

Dentin-bonding agents

Restorative materials

Sealants

Cements

Dentin-bonding agents. Relies on a phosphate- calcium bond for retention of restoration Promotes infiltration of monomers into a zone of demineralized dentin that polymerize and interlock with the dentin matrix .Every product has their own unique system with different variations .

Amalgam. General Description    A mixture of mercury and silver alloy powder that forms a hard solid metal filling. Self-hardening at mouth temperature.

Principal Uses    Dental fillings and heavily loaded back tooth restorations.

Leakage and Recurrent Decay

Leakage is moderate, but recurrent decay is no more prevalent than other materials.

Overall Durability

Good to excellent in large load-bearing restorations.

Cavity Preparation Considerations

Requires removal of tooth structure for adequate retention and thickness of the filling.

Clinical Considerations

Tolerant to a wide range of clinical placement conditions, moderately tolerant to the presence of moisture during placement.

Resistance to Wear Highly resistant to wear.

Resistance to Fracture Brittle, subject to chippin.

Advantages of Amalgam Restoration

- Strong, durable and withstand occlusal forces

- Placed in one visit

- Lower in expense

- Self sealing with minimal to no shrinkage

- Resistance to further decay is high

- Frequency of repair and replacement is low

- Can be used in wet environment (good in pediatrics)

Disadvantages of Amalgam Restorations

- Special handling required for disposal (mercury content)

- Amalgam can darken over time

- Tooth preparation may require removal of some healthy tooth structure

- Rare but possible localized allergic reaction to amalgam

- Short term sensitivity to Hot and    Cold

- Dental composites. General Description A mixture of submicron glass filler and acrylic that forms a solid tooth-colored restoration. Self- or light-hardening at mouth temperature.    The material contains bisGMA, TEGDMA and Procrylat resins.

- Principal Uses

Esthetic dental fillings and veneers.

- Leakage and Recurrent Decay

Leakage low when properly bonded to underlying tooth; recurrent decay depends on maintenance of the tooth-material bond

- Overall Durability

Good in small-to-moderate size restorations.

- Cavity Preparation Considerations

Adhesive bonding permits removing less tooth structure.

- Clinical Considerations

Must be placed in a well-controlled field of operation; very little

tolerance to presence of moisture during placement.

- Resistance to Wear

Moderately resistant, but less so than amalgam.

- Resistance to Fracture

Moderate resistance to fracture in high-load restorations.

- Post-Placement Sensitivity

Occurrence of sensitivity highly dependent on ability to adequately bond the restoration to the underlying tooth.

- Esthetics

Mimics natural tooth color and translucency, but can be subject to staining and discoloration over time.

Advantages.

Color and shading can be matched to existing tooth

Withstands moderate occlusal pressure

Utilized in anterior and posterior regions

Restorations completed in one visit

Moderately resistant to breakage

Permits greater preservation of tooth structure

Low risk of leakage if bonded to enamel

Frequency of repair or replacement is low to moderate

Disadvantages.

Usually wear out more frequently than metal restorations- need to be replaced more frequently

Placement more time consuming

Can not be used in wet environment

More expensive than amalgams

May wear faster than dental enamel

May leak when bonded    on dentinal layer

Types of Composites. Macro filled      8-12 micron

Adaptic, Consise

- Mini filled            1-5 micron

Estilux

- Micro filled      .04-0.1 micron

Durafil VS

- Macro Hybrid    8-12 micron/ 0.04-0.1 micron

Prisma

- Micro- hybrid      1-3micron / 0.04-0.1 micron

Herculite, Charisma

- Total Complete Composite 5-8 m / 1-5m / 0.01-0.1 micron

Prisma, Herculte XRV

Flowable restorative composite is a low viscosity, visible-light activated,    radiopaque,    flowable nanocomposite. The restorative is packaged in syringes. It is available in a variety of tooth-colored shades. The material contains bisGMA, TEGDMA and Procrylat resins. The fillers are a combination of ytterbium trifluoride filler with a range of particles sizes from 0.1 to 5.0 microns, a non-agglomerated surface modified 20nm silica filler , a non-agglomerated surface modified 75nm silica filler,    and a surface modified aggregated zirconia and    silica cluster filler. The aggregate has an average cluster particle size of 0.6 to 10 microns. The inorganic filler loading is approximately 65%by weight (46% by volume).

Indications:

- Class 3 and 5 restorations

- Restoration of minimally invasive cavity preparations (including small, non stress-bearing occlusal restorations)

- Base/liner under direct restorations

- Pit and fissure sealant

- Undercut blockout

- Repair of resin and acrylic temporary materials

Light cured composite (packable). Indications.

-aesthetic restoration of all classes of cavities

-indirect restorations .

Dental Cements:

- Zinc phosphate

- Silicate

- Silicophosphate

- Polycarboxylate

- Glass ionomers-

- Zinc oxide- eugenol

Zinc phosphate cement the one of the oldest and widely used cements, and is commonly used for luting permanent metal restorations and as a base. It is a high-strength cement base, mixed from zinc oxide powder and phosphoric acid liquid.

- Advantages.

- -Inconspicuous appearance.

- -Speed and ease of usage.

- - Sufficient flow to form a thin layer for the cementing of closely adapted crowns, fixed partial dentures, and inlays.

- -Low thermal conductivity beneath a metallic restoration.

- Disadvantages.

- -Low crushing strength

- -Slight solubility in mouth fluids.

- -Opaque material not suitable for visible surfaces.

Dental silicate cement is the product of a reaction between powdered fluorine-containing alumino-silicate glass and a phosphoric acid.

- The cement paste sets and hardens within a few minutes in the mouth, developing a high compressive strength; the set cement is translucent, aesthetic; its thermal expansion matches that of dintine and tooth enamel; a cariostatic action because of its ability to slowly release fluoride ions; has a good resistance towards abrasion. But its chief disadvantage is the staining, erosion and ultimate disintegration it undergoes in oral fluids, brittle nature.

Silicophosphate cement is a mixture of silicate and zinc phosphate cements, formerly used as temporary filling material and for cementation of orthodontic bands, indirect restorations, and porcelain jacket crowns.

Zinc Polycarboxylate Cement. Was one of the first chemically adhesive dental materials, bonding appears to be the result of a chelation reaction between the carboxyl groups of the cement and calcium in the tooth structure.

Composition

Powder

is similar to that of zinc phosphate cement powder, consisting of approximately 90% zinc oxide and 10%

magnesium oxide

Liquid

is an aqueous solution of from 32% to 43% polyacrylic acid of relatively high molecular weight

Zinc Polycarboxylate Cement. Advantages

- kind to the pulp, chemically bonds to tooth structure

Disadvantages

- short working time, requires separate tooth

- conditioning step prior to cementation

- Working time is approximately 2½ minutes, which is half that of

zinc phosphate cement.

- The liquid of this cement tends to be viscous because it is a

partially polymerized polyacrylic acid.

Used for permanent cementation of restorations and appliances. Cementation of orthodontic bands. A base for other filling materials used in restorative procedures. Filling in deciduous teeth. A long term temporary filling

Zinc Oxide-Eugenol Cement. Zinc oxide reacts with water to produce zinc hydroxide which then combines with eugenol to produce zinc eugenolate. Within this matrix are found unreacted zinc oxide powder particles. The fact that zinc eugenolate readily hydrolyzes to form free eugenol and zinc hydroxide accounts for the fact that this is one of the most soluble cements.

Composition

Powder

ZnO 69.0%

white rosin 29.3%

zinc stearate 1.0%

zinc acetate 0.7%

5

Liquid

eugenol 85.0%

olive oil 15.0%

Advantages

- obtundent effect on the pulp

- good short-term sealing

Disadvantages

- weak, soluble

Often used when confronted with multiple areas of excessive decay and sensitivity

- Provides a    *sedative effect*

- Used as a temporary cementation of crowns

- Used to fill obliterated pulp chambers following a pulpotomy

Glass ionomer cement. Mixture of fluoride containing glass powder and organic acid that forms a solid tooth colored restoration able to release fluoride.

Classification of GICs:

-restorative cements (including liner/base materials)

-self-hardening

-partially light-hardening

-metal modified

-resin-modified

-luting cements

-cements for fixation

Clinical Advantages

- Ideal for pediatric and geriatric patients

- Indicated for cervical erosion or lost restorations

- Less shrinkage than traditional composites

- Chemical bond to enamel and dentin

- Coefficient of thermal expansion close to that of enamel and dentin

- High fluoride release

- Radiopaque

- Adhesive bonding permits removing less tooth structure

Clinical disadvantages

- Low resistance to fracture

- Mimics natural tooth color, but lacks natural translucency of enamel

- Little tolerance to presence of moisture during placement

Indications

- Class III and V restorations

- Erosions or Wedge-shaped defects

- Small Class I fillings

- Core build-ups

- Minimally Invasive Dentistry (MID)

Compomers. Clinical advantages

- Good for pediatric patients

- Blend/ combination of resin based composite and glass ionomers

- Combination of Acid+ Base reaction and light activated

- Used with bonding agent – manufacturers say etching of enamel is optional

- Combines wear resistance/ rapid light set 40 seconds/ fracture resistance

- Releases fluoride (glass ionomer property)

5. Materials for students activation during the lecture.

6. General material and methodological ensuring of the lecture

1.Multimedia demonstration.

7. Materials for self-preparation of students

8. Literature.

1.Терапевтическая стоматология детского возраста. Хоменко Л.А., Чайковский Ю.Б., Савичук А.В., Савичук Н.О. и др.// К.:«Книга плюс» - 2013. – p. 203-236.

2.Ніколішин А.К.Терапевтична стоматологія. Том 1// Полтава: «Дивосвіт» - 2012. – p. 75-76.

3.Nikhil Marwah. Textbook of pediatric dentistry.//New Delhi: Jaypee Brothers Medical Publishers. 2011, p. 21-29.

4.Christian H.Splieth. Revolutions in pediatric dentistry //Quintessence Publishing Company, Incorporated: - 2011. – p.2 6-28.

5.David M. Sullivan. Manual of Pediatric dentistry //Lexi-Comp Incorporated,- 2012- p. 38-43.